SECTION 071400

FLUID-APPLIED WATERPROOFING

The highlighted text boxes and anything in blue text is for internal use only. Please delete once the appropriate warranty option is selected.

PART 1 - GENERAL

1.01	RELATED DOCUMENTS

A.	Drawings and general provisions of the Contract, including General and Supplementary Conditions and other Division 1 Specification Sections, apply to this Section.

1.02	SUBMITTALS

A.	Comply with pertinent provisions of Section 01300.

B.	Product Data:  Submit the following:

1.	Materials list of items proposed to be provided under this Section.

2.	Manufacturer's specifications and other data needed to prove compliance with the specified requirements.

3.	Manufacturer's recommended installation procedures which will become the basis for accepting or rejecting actual installation procedures used on the Work.

4.	Written documentation of applicator's qualifications, including reference projects of similar scope and complexity, with current phone contacts of architects and owners for verification.

1.03	QUALITY ASSURANCE

A.	Owner will engage a qualified testing agency to perform all testing and inspection of fluid applied waterproofing installation.

B.	Use adequate numbers of skilled workmen who are thoroughly trained and experienced in the necessary crafts and who are completely familiar with the specified requirements and the methods needed for proper performance of the work of this Section.

C.	Applicator Qualifications:

1.	Applicator shall have at least three years’ experience in installing materials of types specified and shall have successfully completed at least three projects of similar scope and complexity.

2.	Applicator shall designate a single individual as project foreman who shall be on site at all times during installation.

Retain “Independent Observation” Paragraph below if Option 2 under “Warranty” is selected. This is a requirement to obtain AVM Aussie Guard No Dollar Limit Warranty covering both material and labor

- Independent Observation: Owner shall make all arrangements and payments for an independent observation service to verify and approve substrate prior to installation; monitor waterproofing material installation compliance with the project contract documents and manufacturer’s published literature and site-specific details. Independent Observation Firm shall be an approved company participating with the waterproofing manufacturer’s inspection program. Observation service shall produce reports and digital photographs documenting each site visit. Reports shall be made available to the Contractor, waterproofing installer, waterproofing material manufacturer, and Architect. Observations should include substrate examination, beginning of waterproofing installation, periodic intervals, and final observation prior to concrete or backfill placement against the waterproofing.

- Pre-Installation Conference:

- Conduct preconstruction meeting at the project site to review the waterproofing requirements including substrate conditions and pretreatment, surface preparation, minimum curing periods, unique details, sheet flashings, installation procedures, testing and inspection procedures, protection and repair procedures, warranty requirements, and all other work covered under this Section.

- The preconstruction meeting shall occur only after a complete submittal has been submitted, reviewed and approved by the Architect and Owner’s Consultant.

- Attendees shall include the Owner’s Representative or Owner, Architect, Owner’s Consultant, General Contractor, Waterproofing Contractor, Manufactures’ Representative and any other trade Representatives from involved in this scope of work and adjacent work (e.g. shoring installer, concrete subcontractor, etc.).

Schedule Coordination:  Schedule work such that membrane will not be left exposed to weather for longer than that recommended by the manufacturer.

1.04	DELIVERY, STORAGE, AND HANDLING

A.	Comply with pertinent provisions of Section 01600.

B.	Deliver materials to job site in manufacturer's unopened containers with all labels intact and legible at time of use.

C.	Maintain the products in a dry condition during delivery, storage, handling, installation, and concealment. Adhere to manufacturer’s Delivery, Storage and Handling requirements.

1.05	SUBSTRATE CONDITIONS

A.	Provide applicator with substrates that are free of standing water, dirt and debris, loose material, voids and protrusions or deformations which may inhibit application or performance of waterproofing.

1.	Where work of this Section will be installed on concrete and/or masonry, provide substrates that are free of voids deeper than 3/8" and free of surface protrusions more than 1/4" above the surface. Grind/remove all sharp edges.

2.	Where work of this Section will be installed on concrete footings, provide wood float or better finish to surfaces scheduled to receive the membrane.

3.	Where work of this Section will include bentonite waterstop strips, provide concrete surfaces as required for that installation.

4.	Carefully follow manufacturer’s detailing procedures, recommendations and details for proper waterproofing of penetrations.

1.06	WARRANTY

.

Warranty Selection: Below are two warranty options offered by AVM Industries. The selection of Option #2 will involve additional requirements mentioned throughout the paragraph. Delete the option NOT selected.

If Shotcrete is being used for structural foundation walls and the project is beneath the water-table (hydrostatic condition), please consult with your AVM representative prior to finalizing the specification.  AVM’s dual waterproofing system may be required.

Option #1 (A): Remove paragraph below if Option #2 is selected

- Manufacturer’s Warranty:  Manufacturer's standard form in which waterproofing manufacturer agrees to furnish waterproofing material to repair or replace those materials installed according to manufacturer's written instructions that exhibit material defects or otherwise fail to perform as specified under normal use within warranty period specified.

  - Access for Repair: Owner shall provide unimpeded access to the Project and the waterproofing system for purposes of testing, leak investigation, and repair, and shall reinstall removed cladding and overburden materials upon completion of repair.

  - Cost Limitation: Manufacturer’s obligation for repair or replacement shall be limited to the original cost of the material

  - Warranty Period: 5 years from date of Substantial Completion

  - Applicator will provide a 2-year labor

Option #2 (B): Remove paragraph below if Option #1 is selected

- Manufacturer’s Warranty:  Upon installation completion and manufacturer acceptance of the work required by this section, the waterproofing materials manufacturer will provide to the project Owner, a written ten (10) year No Dollar Limit AussieGuard® waterproofing warranty, covering both materials and labor.  Issuance of Manufacturer's Waterproofing Warranty requires the following:

  - Waterproofing system products shall have been provided by a single manufacturer

  - Pre-Installation Conference.  Reference Section  1.04 (Quality Assurance), Section E

  - Installation inspected by an approved 3rd Party Independent Inspection Firm. Reference 1.04 (Quality Assurance), section C (Independent Observation).

  - Waterstop manufactured and supplied by the waterproofing membrane manufacturer must be installed in all applicable concrete construction joints and around applicable penetrations.  Reference Specification Section 031500- Waterstops

  - Applicator will provide a 2-year labor warranty.

PART 2 - PRODUCTS

2.01	MATERIALS

- Fluid-Applied Waterproofing:

AVM Aussie Membrane 500, Single component Bitumen	ICC ESR-2503, LARR 25550

  - For Retaining Walls, use:	Aussie 500

  - For Planters, use:		Aussie 500

  - For Between Slab, use:	Aussie 500

B.	Primer:  As recommended by waterproofing membrane system manufacturer;

C.	Joint backing:  Closed-cell, polyethylene rod as recommended by membrane manufacturer.

D.	Reinforcing fabric:  As recommended by manufacturer.

E.	Protection Course:

- Retaining Walls:	AVM Drain Board 6000

2.	Planters:  		AVM Drain Board 6000.

3.	Between Slabs:	AVM Drain Board 6000 or Drain Board 9000.

F.	Sealant:  Aussie Seal M.

2.02	MATERIAL SPECIFICATIONS

Aussie Membrane 500 Specifications: Single component roller applied bitumen

(ICC ESR-2503, LARR 25550)

| Technical Information |  |  |
| --- | --- | --- |
| Color | Dark brown. After drying: black |  |
| Specific Gravity | 1.189 gr/cm² |  |
| Coverage: (Varies depending on substrate) | 18–19 sq.ft./Gal. @ 60 Dry Mills |  |
| Flash Point | Non-flammable |  |
| Service Temperature | 15ºF-177ºF (-10ºC to +80ºC) |  |
| Application Temperature | 42ºF-132ºF (+5ºC to 55ºC) |  |
| Solid Content | 64% |  |
| Tensile Strength | >15.4 Lbs (>7 kg) | ASTM D 412 |
| Elongation at break | >1000% | ASTM D 412 |
| Resistance to water pressure 1 tm 24 hr | Passed | ASTM D751 |
| Water vapor transmission | 4.0 gr/m² 24 hr | ASTM D 96 |
| Recovery | 85% | IS 1536 |
| Creep At 177ºF (80ºC) | No Creep | DIN 52123 |
| Resistance to Standing Water | Passed | ASTM D 2939 |
| Bacterial Attack in soil 30 days @ 105ºF (40ºC) | Passed | ASTM D 2939 |
| Crack bridging | >3/16" (>5mm) | IS 1731 |
| Certifications | ISO 9002, Green Label, I.Q. Net (International Certification Network) |  |

2.03	OTHER MATERIALS

- Provide other materials, not specifically described but required for a complete and proper installation, as selected by the Contractor subject to the approval of the Architect.

PART 3 - EXECUTION

3.01	SURFACE CONDITIONS

A.	Examine the areas and conditions under which work of this Section will be performed.

1.	Verify conformance with manufacturer's requirements.

2.	Report unsatisfactory conditions in writing to the Architect.

3.	Correct conditions detrimental to timely and proper completion of the Work.  Do not proceed until unsatisfactory conditions are corrected.

B.	Coordinate as required with other trades to assure proper and adequate provision in the work of those trades for interface with the work of this Section and to prevent damage to installed waterproofing.

C.	Commencement of installation of any products of this Section shall be considered as acceptance of the substrate and conditions as being satisfactory for proper installation of products of this Section.

3.02	PREPARATION

A.	Surface preparation and detailing procedures to be in accord with waterproof membrane system manufacturer's instructions and recommendations except where more stringent requirements are indicated.

B.	Clean all surfaces to receive membrane system in accord with manufacturer's instructions; vacuum clean or blow clean with oil-free compressed air all surfaces to receive sealants, detailing materials or membranes immediately prior to installation.

C.	Rout, clean, prepare and detail surface cracks in accord with manufacturer's instructions; install backer rod where required.

D.	Clean metal surfaces to bright metal by wire brushing or mechanical etching; scuff-sand lead flashing and plastic surfaces.

E.	Prime surfaces in accord with manufacturer's instructions.

F.	Install detail coats, joint, crack and transition treatments in accord with manufacturer's instructions and details.

G.	Allow detail applications to cure in accord with manufacturer's instructions prior to general application of membrane.

3.03	INSTALLATION

A.	Coordinate as required with other work to assure proper and adequate provision in other work for interface with the work of this Section.

B.	Install the work of this Section in strict accordance with the original design, pertinent requirements of governmental agencies having jurisdiction, and the manufacturer's recommended installation procedures.

1.	Waterproofing membrane average dry-film thickness per manufacturer's specifications.

2.	Grid deck surfaces to assure proper coverage rates and verify membrane wet-film mil thickness with gauges as work progresses.

3.	Retain empty product containers during course of work to aid in determining whether completed membrane complies with required average dry-film thickness.

C.	Verify proper dry condition of substrate using method recommended by membrane system manufacturer; perform adhesion checks prior to general application of membrane system using field adhesion test method recommended by manufacturer.

C.	Mask off adjoining surfaces not to receive membrane system.

D.	Apply membrane uniformly and allow to cure in accord with manufacturer's instructions.

E.	Feather terminating edge when entire area cannot be completed in one day; clean area 6" wide along terminating edge of membrane prior to startup on next working day; Follow  manufacturer's instructions as needed; overlap existing work by 6" with new work.

F.	Flood test:  Plug drains on deck surfaces and use sand bags or other means to restrict runoff.  Flood deck with water to depth of 2" (50 mm) and allow to stand at least 48 hours; repair leaks if occurs and retest.

G.	Install drainage board over cured membrane in accord with manufacturer's instructions.

3.04	PROTECTION AND CLEAN-UP

A.	Promptly remove primer or membrane system material from adjacent surfaces. Leave work area in broom clean condition.

B.	Prohibit traffic over completed work and protect against work overhead until protection course is installed; protect from damage until protected beneath overlaying work.

END OF SECTION 071400